NORI 40 FSL/FSS

Short text:

Y-pattern strainer made of cast steel 1.0619+N (GP 240 GH+N), with standard screen, with flanged ends or butt weld ends, face-to-face length to DIN EN 558-1/1 (flanged ends) or EN 12982 (butt weld ends).

Manufacturer/Type:		KSB/NORI 40 FSL/FSS

Pressure class:	PN 25/40

Nominal size:	DN 15-300

Long text:

Y-pattern strainer made of cast steel 1.0619+N (GP 240 GH+N), with standard screen, with flanged ends or butt weld ends, face-to-face length to DIN EN 558-1/1 (flanged ends) or EN 12982 (butt weld ends), -10 °C to 450 °C, with drain plug in the cover, fully confined cover gasket, free from non-ferrous metals, exterior coating of high-temperature resistant paint (grey aluminium). Designed, manufactured, tested and marked in acc. with the European Pressure Equipment Directive. For use in potentially explosive atmospheres, Group II, category 2 (zones 1 and 21) and category 3 (zones 2 and 22) to ATEX 2014/34/EU.

Manufacturer/Type:		KSB/NORI 40 FSL/FSS

Pressure class:	PN 25/40

Nominal size:	DN 15-300

Variants:

with fine screen

or

with magnetic insert (max. 300 °C)

or

with studs and nuts made of A4-70 (low-temperature steel down to -30 °C)

or

other types of flange or weld end designs

Typical tender for NORI 40 FSL/FSS

7127.521/01-EN
Subject to technical modification without prior notice

19 April 2021