NORI 40 ZYLB/ZYSB

Short text:

Metal-seated Y-pattern globe valve with double-walled bellows, with flanged ends or butt weld ends, body made of cast steel 1.0619+N (GP 240 GH+N), face-to-face length to DIN EN 558-1/1 (flanged ends) or EN 12982 (butt weld ends).

Manufacturer/Type:		KSB/NORI 40 ZYLB/ZYSB

Pressure class:	PN 25/40

Nominal size:	DN 15 - 300

Long text:

Metal-seated Y-pattern globe valve with double-walled bellows, maintenance-free, with flanged ends or butt weld ends, body made of cast steel 1.0619+N (GP 240 GH+N), face-to-face length to DIN EN 558-1/1 (flanged ends) or EN 12982 (butt weld ends), -10 °C to 450 °C, with position indicator, locking device and travel stop as standard, with throttling plug up to DN 100, with double-walled bellows made of 1.4571 and back-up gland packing, replaceable valve disc, non-rotating stem made of 1.4021, hard-faced seat, fully confined bonnet gasket, exterior coating of high-temperature resistant paint (grey aluminium), free from non-ferrous metals. Designed, manufactured, tested and marked in acc. with the European Pressure Equipment Directive. For use in potentially explosive atmospheres, Group II, category 2 (zones 1 and 21) and category 3 (zones 2 and 22) to ATEX 2014/34/EU.

Manufacturer/Type:		KSB/NORI 40 ZYLB/ZYSB

Pressure class:	PN 25/40

Nominal size:	DN 15 - 300

Variants:

with throttling plug from DN 125

or

with balanced plug from DN 125

or

with studs and nuts made of A4-70 (low-temperature steel down to -30 °C)

or

with limit switch

or

other types of flange or weld end designs

Typical tender for NORI 40 ZYLB/ZXSB

7160.521/01-EN
Subject to technical modification without prior notice

19 April 2021