NORI 40 ZXLB/ZXSB

Short text:

Metal-seated globe valve in straight-way pattern, with double-walled bellows and two-piece stem,

model with flanged ends: face-to-face length to DIN EN 558/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 200 made of 1.0619+N (GP 240 GH+N)

model with butt weld ends: face-to-face length to EN 12982/64,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 200 made of 1.0619+N (GP 240 GH+N),

Manufacturer/Type:		KSB/NORI 40 ZXLB/ZXSB

Pressure class:	PN 25/40

Nominal size:	DN 10 - 200

Long text:

Metal-seated bellows-type globe valve, maintenance-free

Model with flanged ends: face-to-face length to EN 558/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 200 made of 1.0619+N (GP 240 GH+N)

Model with butt weld ends: face-to-face length to EN 12982/1,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 200 made of 1.0619+N (GP 240 GH+N),

-10 °C to +450 °C, straight-way pattern, rotating upper stem made of 1.4021, non-rotating lower stem made of 1.4122 with back seat, fully confined bonnet gasket, with handwheel, with position indicator, stem sealed by double-walled bellows made of 1.4571 and back-up gland packing, bellows welded to stem,

plug-type replaceable valve disc, free from non-ferrous metals. Designed, manufactured, tested and marked in acc. with the European Pressure Equipment Directive. For use in potentially explosive atmospheres, Group II, category 2 (zones 1 and 21) and category 3 (zones 2 and 22) to ATEX 2014/34/EU.

Manufacturer/Type:		KSB/NORI 40 ZXLB/ZXSB

Pressure class:	PN 25/40

Nominal size:	DN 10 - 200

Variants:

with throttling plug

or

with balanced plug (from DN 125)

or

with locking device / travel stop

or

studs and nuts made of A4-70 (low-temperature steel)

or

oil and grease-free

or

with leakage detection hole

or

seal-welded body/bonnet joint

or

other types of flange or weld end designs

Typical tender for NORI 40 ZXLB/ZXSB

7165.521/01-EN
Subject to technical modifications

19 April 2021