NORI 40 ZXLF/ZXSF

Short text:

Metal-seated globe valve in straight-way pattern, with gland packing and non-rotating stem,

model with flanged ends: face-to-face length to EN 558-1/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 200 made of 1.0619+N (GP 240 GH+N)

model with butt weld ends: face-to-face length to EN 12982/64,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 200 made of 1.0619+N (GP 240 GH+N),

Manufacturer/Type:		KSB/NORI 40 ZXLF/ZXSF

Pressure class:	PN 25/40

Nominal size:	DN 10 - 200

Long text:

Metal-seated globe valve with gland packing and non-rotating stem,

model with flanged ends: face-to-face length to EN 558-1/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 200 made of 1.0619+N (GP 240 GH+N)

model with butt weld ends: face-to-face length to EN 12982/64,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 200 made of 1.0619+N (GP 240 GH+N),

-10 °C to +450 °C, straight-way pattern, non-rotating stem made of 1.4021 with back seat, fully confined bonnet gasket, with handwheel, with position indicator, stem sealed by gland packing. Designed, manufactured, tested and marked in acc. with the European Pressure Equipment Directive. For use in potentially explosive atmospheres, Group II, category 2 (zones 1 and 21) and category 3 (zones 2 and 22) to ATEX 2014/34/EU.

Manufacturer/Type:	KSB/NORI 40 ZXLF/ZXSF

Pressure class:	PN 25/40

Nominal size:	DN 10 - 200

Variants:

with electric actuator

or

with single-piece stem and throttling plug assembly

or

with balanced plug

or

with locking device

or

with PTFE gland packing

or

oil and grease-free

or

studs and nuts made of A4-70 (low-temperature steel)

or

with limit switch

or

other types of flange or weld end designs

Typical tender for NORI 40 ZXLF/ZXSF

7622.521/01-EN
Subject to technical modification without prior notice

19 April 2021