NORI 40 RXL/RXS

Short text:

Metal-seated lift check valve in straight-way pattern, with spring-loaded valve disc,

model with flanged ends: face-to-face length to EN 558-1/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 300 made of 1.0619+N (GP 240 GH+N)

model with butt weld ends: face-to-face length to EN 12982/64,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 300 made of 1.0619+N (GP 240 GH+N),

Manufacturer/Type:		KSB/NORI 40 RXL/RXS

Pressure class:

PN 25/40

Nominal size:

DN 10 - 300

Long text:

Metal-seated lift check valve with spring-loaded valve disc

Model with flanged ends: face-to-face length to DIN EN 558-1/1,

DN 10 - 40 body made of 1.0460 (P 250 GH), DN 50 - 300 made of 1.0619+N (GP 240 GH+N)

Model with butt weld ends: face-to-face length to EN 12982/64,

DN 10 - 50 body made of 1.0460 (P 250 GH), DN 65 - 300 made of 1.0619+N (GP 240 GH+N),

-10 °C to +450 °C, straight-way pattern, fully confined cover gasket. Designed, manufactured, tested and marked in acc. with the European Pressure Equipment Directive. For use in potentially explosive atmospheres, Group II, category 2 (zones 1 and 21) and category 3 (zones 2 and 22) to ATEX 2014/34/EU.

Manufacturer/Type:		KSB/NORI 40 RXL/RXS

Pressure class:

PN 25/40

Nominal size:	DN 10 - 300

Variants:

Studs and nuts made of A4-70 (low-temperature steel)

or

oil and grease-free

or

other types of flange or weld end designs

Typical tender

NORI 40 RXL/RXS

7673.521/01-EN
Subject to technical modification without prior notice

16 April 2021